**Seam Sealing Directions Using SU 106**

1. *If installing Flex-Floors Extreme, be certain that seams are double-cut.*
2. Before beginning, be certain that seams are clean and dry.
3. Shake Part B to blend flattening additives.
4. Empty the entire contents of Parts A and B into the plastic squeeze bottle. Securely tighten applicator nozzle and gently shake mixture. Wait for air bubbles o disappear (about 10 minutes) before continuing.
5. Insert the slotted fin into the seam cut at one end of the seam. Squeeze the plastic bottle with light pressure and apply a continuous bead of seam sealer 1/8” – 3/16” wide centered on the seam cut. Move slowly with as few interruptions as possible.
6. SU106 Seam Sealer will be dry to the touch in about 2 hours. However, the seam must be protected for at least 16 hours to allow for complete drying. The trimmed-off selvage edge from the seam cut can be taped parallel with the seam to warn people about the wet seam sealer.